Section 08 3493

AUTOMATIC overhead coiling fabric Fire Curtain

# General

## Summary

### Section Includes:

#### Fire alarm or smoke detector-activated, overhead coiling fabric fire curtain.

#### Self-closing without auxiliary power.

#### For complex, large and small protected openings.

### Related Requirements:

#### 08 3100(Access Panels.

#### 09 2200( Load bearing header framing

#### 09 9100(Paint: Field painting of specified components.

#### 28 3000(Detection and Alarm: Provision of smoke detectors.

#### Division 26 Sections for 120VAC (10 amp service with disconnect) control circuit power including conduit, boxes, conductors, wiring devices, and emergency power.

## References

### NFPA Codes and Standards:

#### 70 ( National Electrical Code.

#### 72 – National Fire Alarm Code -2007, 2010 and 2013.

#### ASTM - E84 - Test Method for Surface Burning Characteristics of Building Materials

### UL Standards:

#### 268 ( Smoke detectors for fire protective signaling systems.

#### 864 ( Control units for fire protective signaling systems.

#### 10B – Fire tests for door assemblies.

#### 10C – Positive pressure fire tests for door assemblies.

#### 10D – Fire tests for fire protective curtains.

#### 1784 – Air leakage tests for door assemblies.

## SUSTAINABLE DESIGN REQUIREMENTS

### LEED-NC: Comply with Section 01 8100 sustainable design requirements including, without limitation, submittal and documentation requirements.

### Credit/Point Goals Applicable To This Section: In addition to global project credit/point goals:

#### Materials & Resources - construction waste management

#### Materials & Resources - recycled content

#### Materials & Resources - regional materials

#### Indoor Environmental Quality - construction IAQ management plan

## submittals

### Comply with Section 01 3300(Submittal Procedures:

#### Product data.

#### Shop drawings:

##### Include opening dimensions.

##### Show and identify related work performed under other sections of the specifications.

#### Quality Assurance/Control Submittals:

##### Certifications.

##### Manufacturer’s installation instructions and testing procedures.

## closeout submittals

### Comply with Section 01 7700(Project Closeout:

#### Operation and maintenance manual.

#### Manufacturer’s warranty.

## Quality Assurance

### Certifications:

#### ETL Listing to UL standards:

##### 864 - Control units for fire protective signaling systems.

##### 268 - Smoke detectors for fire protective signaling systems.

##### 10B (20 minutes) - Fire tests for door assemblies.

##### 10C (20 minutes) - Positive pressure fire tests for door assemblies.

##### 10D (2 hours) - Fire tests for fire protective curtains.

##### 1784 - Air leakage tests of door assemblies.

### Pre-Installation Meeting:

#### Schedule and convene a pre-installation meeting prior to commencement of field operations with representatives of the following in attendance: Owner, Architect, General Contractor, fire curtain sub-contractor, and electrical sub-contractor.

#### Review substrate conditions, requirements of related work, installation instructions, storage and handling procedures, and protection measures.

#### Document the responsibilities of various parties and deviations from specifications and installation instructions.

## Delivery, Storage, and Handling

### Comply with Section 01 6600(Delivery, Storage, and Handling.

### Comply with manufacturer’s instructions.

## Warranty

### Provide manufacturer’s standard one year warranty.

### Maintenance and Testing:

#### Perform minimum semi-annual maintenance and testing on each fire curtain as required by the manufacturer’s warranty, code agency evaluation reports, and as required by local authority having jurisdiction.

#### Provide test documentation.

# Products

## ManufactureD  units

### Model M2500.

### Manufacturer:

#### Smoke Guard, Inc.

#### Distributed by Smoke Guard, 287 N. Maple Grove, Boise, Idaho  83704 www.smokeguard.com/

### Label each fire curtain with following information:

#### Manufacturer’s name.

#### Label of quality control agency.

## Performance / DESIGN CRITERIA

### Test normal and fire operation: Curtain to deploy on activation of building fire alarm system signal or test key switch. Curtain shall descend and rewind by motor drive.

#### Raise curtain after test and after fire alarm is cleared.

#### Reset curtain after test or operation of unit using key switch. No manual reset required. No service call needed. No replacement parts needed.

### Test to 6,000 cycles.

## Components

### Curtain Fabric:  SG Tex 30 - Glass fiber material with steel wire reinforcement that is coated on both sides with a polyurethane.

### Side Guide Assembly:

### Housing/Bearing Type:  Standard or support bearing.

### Bottom Bar: Weighted for self-closing by gravity.

### Rewind Motor:

#### Tubular motor with fail safe gravity deploy operation.

#### 24 VDC.

### Control System:

#### Comply with UL Standard 864.

#### Battery backup supplied with the controls.

#### 120 VAC power

### Finishes:

#### Manufacturer’s standard galvanized finish.  Optional finishes available at extra cost including: field painting, stainless steel or powder coat.

## fabrication

### Installation Configuration:  Housing attached directly to substrate above opening or to wall.

### Fabricate and install mounting brackets, hardware, and fasteners needed to attach fire curtain assembly to building structure.

# Execution

## Examination

### Examine substrates upon which work will be installed.

#### Verify related work performed under other sections is complete and in accordance with shop drawings.

#### Verify wall surfaces are acceptable for installation of fire curtain system components.

### Coordinate with responsible entity to perform corrective work on unsatisfactory substrates.

### Coordinate electrical interface and connection with Division 26.

### Coordinate interface and connection with fire and alarm system.

### Commencement of work by installer is acceptance of substrate.

## INSTALLATION

### Install fire curtain system components in accordance with manufacturer’s installation instructions.

## Field Quality Control

### Field Test: Follow manufacturer’s cycle test procedures.

#### Notify Owner’s Representative, local Fire Marshal and alarm sub-contractor minimum one week in advance of scheduled testing.

#### Complete maintenance service record.

## Demonstration

### Demonstrate required testing and maintenance procedures to Owner’s Representative.

End of Section

# Text boxes

See manufacturer’s literature for types of side guides.

See manufacturer’s literature for side guide style and dimensions.

See manufacturer’s literature for alternate types of housing attachments.